| TECHNICAL DATA SHEET SERIES 650 GEO Water Based In-Mould-Coating For PU - Grip/Rubber Effect |
| --- |
| KEZAL 650/…GEO |
| DESCRIPTION | Water based mono-component in-mould-coating varnish for PU |
| CHARACTERISTICS | Liquid water based Gives the PU a rubber effect Higher adhesion to the ground |
| APPLICATION | Clean well the mould Shake before using Mould temperature 50-65 °c minimum Spray using nozzle gun diam. 0.5 mm Spray the product at pressure 2.5 bar Spray the product directly into the mould after the release agent 710/... |
| ADVANTAGES | No solvent content Environmental friendly product Small quantity No need to use the spray machine Elimination of cream lines and pouring marks No need to wash and decrease of colouring paste utilization |
| COLOURS | All colours |
| PACKING | Plastic cans of 20 lt. Plastic drums of 100-200 lt. |
| STORAGE | Keep in well closed original packing in a dry and airy place. Shelf life 12 months. Avoid extreme cold-heat (preferably +5/30 °c) |