| ### TECHNICAL DATA SHEET SERIES 650 GEO - Water Based In-Mould-Coating For PU - Grip/Rubber Effect |  |
| --- | --- |
| ## KEZAL 650/…GEO |  |
| DESCRIPTION | Water based mono-component in-mould-coating varnish for PU |
| CHARACTERISTICS | - Liquid water based - Gives the PU a rubber effect - Higher adhesion to the ground |
| APPLICATION | - Clean well the mould - Shake before using - Mould temperature 50-65 °c minimum - Spray using nozzle gun diam. 0.5 mm - Spray the product at pressure 2.5 bar - Spray the product directly into the mould after the release agent 710/... |
| ADVANTAGES | - No solvent content - Environmental friendly product - Small quantity - No need to use the spray machine - Elimination of cream lines and pouring marks - No need to wash and decrease of colouring paste utilization |
| COLOURS | All colours |
| PACKING | - Plastic cans of 20 lt. - Plastic drums of 100-200 lt. |
| STORAGE | - Keep in well closed original packing in a dry and airy place. - Shelf life 12 months. - Avoid extreme cold-heat (preferably +5/30 °c) |